Lotus Europa S2 – Zetec Motor Mounts

Decided to recast my stock motor mounts rather than replace them with new mounts.  Thought I would try a two part product for making rubber parts and solve a small issue with the mount orientation.  Since I am installing a Zetec, I thought it best of the motor mount tabs faced perpendicular to the motor, rather than parallel to the chassis “Y”. I am sure Lotus avoided this issue originally so they could use non-handed parts.

Here is how they started out.  Lots of dry cracking.

Step one: Using a hack saw, cut along all sides of the metal mount.  You can then separate the inner mount from the cradle.  I then used a wire wheel to finish up removing the loose rubber.

Step two: Create a complete watertight chamber for pouring the rubber.  This is easily done by using some aluminum tape along the back and top of the mount cradle.

Step three: Mix and pour the two part rubber solution.  Contact www.jgreer.com. for info about the Shore 75A product.

Step four: Wait 20 minutes and remove the foil tape and you are done.  All that is needed from here on out is a nice coat of paint.  The bottles recommend waiting 24 hours before use.

All this took me about an hour from start to finish.  I am sure that if you were setting up a small production line you could cut this time in half.

I’ll have to let you know how they hold up in real use…

Dean (HealeyBN7@yahoo.com)